## Slide 1
Nuclear Fission Research infrastructure needs and access schemes in Belgium
Hamid AÏT ABDERRAHIM
Deputy Director-General
haitabde@sckcen.be
Forum on access to existing EU nuclear fission research infrastructure
January 29, 2015, Brussels (BE)

## Slide 2: Outline
Nuclear Fission Research infrastructure needs in Belgium
Few examples of Nuclear Fission RI accessible in Belgium
Other institutions in Belgium useful RI for Nuclear Fission
Nuclear Fission RI access right in Belgium
Issues for Nuclear Fission RI to be addressed at EC level

## Slide 3: Nuclear Fission Research infrastructure needs in Belgium
Material testing and qualification
  Fission Reactors : Gen.II, III and IV
  Fusion Demo
  Ceramic advanced materials
Fuel development, testing, validation and qualification
  MTR HEU  LEU
  NPP: Gen.II & III
  FR Gen.IV
  Advanced Fuels for Transmutation
LTO
  Structural materials
  Cables aging
  Concrete aging
RI production:
  new material targets development and qualification

## Slide 4: BR2 Material Testing Reactor

## Slide 5: BR2 at a glance: 8 is the magic number
Aluminum pressure vessel, pressure 1.2 Mpa
~ 800 mm core height
~ 80 irradiation channels composed of Beryllium and stainless steel
Access from top (all channels) and bottom
(8 inch and some 3.5 inch channels)

## Slide 6: BR2 Core characteristics
Neutron flux range (variable with configuration)
  Thermal 1014 n/cm²s to 1015 n/cm²s
  Fast (E>0.1MeV) 1.5 1013 n/cm²s to 6 1014 n/cm²s
Fuel:
  Metallic MTR fuel: dispersed UAl alloy in Al matrix
  5-6 concentric plates
  Maximum heat flux 470W/cm², 600W/cm² in experiments
Moderator:
  Solid Be metal
  Light water
Absorber:
  Hf metal

## Slide 7: BR2 a very high flexibility
Core configuration is very flexible in order to combine multiple irradiation devices in one core load
Irradiation devices typically loaded
  Production device for radio-isotopes by fission
  Production device for RI by activation
  Simulation loop of other reactors (PWR - MTR)
  Irradiation of Si

## Slide 8: BR2 Catalogue of applications
Evaluation of safety of nuclear installations
  Irradiation of fuel: safety margin in normal/accidental conditions
  Irradiation of structural materials: qualification of new materials and ageing of reactors
  Testing of instruments under irradiation: diagnostics of nuclear installations
Contribution to public health & environment protection
  Irradiation services to produce radio-isotopes for nuclear medicine and industry (safety of industrial installations)
  Supporting development of renewable energy and energy lean technology by supplying high quality semi-conductors for high power applications through irradiation of Si
Reducing the risk of nuclear proliferation
  By qualification of low enriched uranium alternatives to current day’s high enriched uranium based applications in MTRs

## Slide 9: Simulation of PWR in BR2: CALLISTO

## Slide 10: BR2 production of Radioisotopes
Application of RI
    Nuclear medicine (diagnostics and therapy …); 30-40M procedures annually worldwide
    Industry (radiography, sterilisation, measurements, …)
    Fundamental research (biology, chemistry, pharmacy…)
BR2 is qualified to supply following isotopes:
    99Mo (99mTc), 131I, 133Xe, 192Ir, 186Re, 153Sm, 90Y, 32P, 203Hg, 188W (188Re), 82Br, 41Ar, 125I, 177Lu, 89Sr, 60Co, 169Yb, 147Nb, …

## Slide 11: Production of semi-conductors by irradiation
Principle of doping - transmutation: 30Si(n,γ)31Siβ-31P.
2 installations in BR2:
  SIDONIE: inside vessel for crystal diameter 3-5”
  POSEIDON: in pool for 6-8”
Capacity of 15 et 18 tonnes annually respectively
Applications of NTD Si: transport (electric and hybride vehicles), renewable energy (solar & wind)

## Slide 12: POSEIDON: Production of doped Si out of core

## Slide 13: BR1 : Natural Uranium – Air - Graphite
Research Reactor
Natural Uranium - Gas - Graphite
In operation since 1956
4 MW Thermal power
Operation
  Daily basis (7h/day)
  700 kW

## Slide 14: BR1 Major Applications & Use
Activation
  Neutron Activation Analysis
  Activation of materials
Qualification of sensitive components
  Sensors, Fibre Optics, Electronics
  In-situ and on-line monitoring
Calibration of detectors
Education & Training
  SCK•CEN
  Electrabel
  Universities & High Schools
Industries (Nat. & Int.)
  Chemical
  Electronics
  Nuclear Instrumentation
Universities & High Schools
Research Institutes
Internal R&D Projects

## Slide 15: Various Irradiation channels available
X & Y Channels
  Parallel or perpendicular to fuel channels
  thermal flux up to 3.5 1011 n/cm².s
Large Cavity
  Thermal spectrum (7 108 n/cm².s)
  Converters
Pneumatic Rabbits
Neutronography
Reactor Core
(natural U)
Graphite
1 m
1 m
Pneumatic rabbits
Irradiation
Channels
Large Cavity

## Slide 16: Si @ BR1 700 kW

## Slide 17: Large Cavity (Thermal Column) - Spherical Drivers
Concrete gamma & neutron shielding
Graphite
Natural uranium
Fe or Cu
Access plug
1 m Cavity

## Slide 18: Pneumatic Rabbits
To allow short time irradiation without shut down
6 “slow” rabbits
1 “fast” rabbit
  Transfer time < 0.8 s

## Slide 19: Lab for High & Medium level Activity: glance view

## Slide 20: LHMA: equipment and activity
Hot cell laboratory to study irradiated reactor materials and nuclear fuels.
Test infrastructure consists of mechanical, chemical and microstructural research instruments
Focus on the analysis of the damage and ageing processes of materials, fuel performance studies, innovative fuel development, testing and qualification
Notch impact test in a hot cell
Hot cell operator at work
Material testing in PbBi in a hot cell

## Slide 21: Access to hot cell infrastructure can be a challenge
Test equipment in non-controlled area:
  Access relatively easy
  Common procedure to enter SCK•CEN site
  Administrative procedure is limited
  Short visits possible
  Organized through YOP (Young Potentials Database) of SCK•CEN Academy
Test equipment in controlled area:
  Access heavy in terms of administrative work
  Extensive screening required (FANC)
  Time consuming process (3 months, sometimes more)
  More interesting for longer visits
  Organised through YOP (Young Potentials Database) of SCK•CEN Academy

## Slide 22: Radiochemistry laboratories for R&D and radio-analytical applications
Laboratories in controlled areas equipped to handle
a wide variety of materials of the nuclear fuel cycle
and related research
Sample preparation for analysis: chemical laboratories, glove boxes, lead shielded cells
Analytical techniques for radionuclide, isotopic and elemental analyses  matrix and trace impurities
  alpha-, gamma- and beta-spectrometry
  Mass-spectrometry dedicated to isotopic and elemental analysis  Thermal Ionization-MS, Inductively Coupled Plasma-MS (quadrupole + high-resolution)
  Chemical analysis  ICP-AES (spectrometric), ion-chromatography, total organic carbon, electrochemistry, etc.

## Slide 23: Nuclear chemistry expertise and capabilities
Qualification unirradiated nuclear fuels
  Matrix elements, trace impurities
  Isotopic compositions and concentration,
  Safeguards
Spent fuel examination
  Destructive burnup analysis
  Spent fuel characterization for code validation
R&D samples related to the nuclear fuel cycle research
  Support to Myrrha: a.o. lead-bismuth eutectic
  radioactive waste disposal in clay formation
  Nuclear fuel development
Operational samples from nuclear facilities
  Radioactive waste characterization from exploitation and dismantling activities
  Evaluation water chemistry
  Reactor materials

## Slide 24: Environment, Health and Safety

## Slide 25: Liquid Heavy Metal Complex - MYRRHA R&D programme
LiLiPuTTeR-II
HELIOS 3
Heavy Liquid Metal Lab
MEXICO
CRAFT
LIMETS 3
RHAPTER
COMPLOT
ESCAPE (1/5 scaled MYRRHA)
Ultrasonic lab
Materials
LBE conditionning
Component testing & TH
Instrumentation
Green: operational, Black: under construction

## Slide 26: MEXICO LBE loop
  over 2000 h of experiment time, 20.106 kg LBE circulated
pilot-scale demonstration of oxygen control technologies:
PbO mass exchanger and electrochemical pumping
accurate & stable oxygen control of 7000 kg of LBE
oxygen control ON
MEXICO loop

## Slide 27: COMPLOT LBE loop
hydraulic and hydrodynamic behaviour of full-scale MYRRHA components in LBE: fuel assembly, spallation target, control and safety rods
commissioning and hydraulic characterisation of instrumentation and equipment with a flow rate of 75 kg/s at 200 °C
COMPLOT
Fuel mock-up
Pump efficiency
COMPLOT

## Slide 28: MYRRHA - Accelerator Driven System Next Large RI at SCK•CEN for European users
Reactor
Subcritical or Critical modes
65 to 100 MWth
Accelerator
(600 MeV - 4 mA proton)
Fast
Neutron
Source
Spallation Source
Lead-Bismuth
coolant
Multipurpose
Flexible
Irradiation
Facility
Innovative & Unique

## Slide 29: MYRRHA A pan-European, innovative and unique facility at Mol (BE)

## Slide 30: MYRRHA Access rules for future users
OPERATION PHASE
Members of Consortium
Individual research of a member of Consortium
Collaborative research amongst members of Consortium
- 3 years program commitment
CLOSED/
SHARED
INFORMATION
for MoC
Open User Facility
Governments funding
Criteria of research excellence
Independant program access committee (PAC)
Collaborative research
- Distribution of information to participants
Contract research…..
Commercial services
RI
NTD Silicon
~25%
~25%
~25%
~25%
OPEN INFORMATION
SHARED INFORMATION
for participants
CLOSED
INFORMATION
for participants
«?» (*)
(*) Statutes under analysis for Phase 2
BENEFITS for Members of Consortium
Board position to control overal operation
Priority of access
Potential benefit of low price (compensation profit from commercial revenues)
Capacity transfer flexibility (rules tbd)
SCK•CEN
as qualified and licenced operator of the MYRRHA infrastructure under contractual arrangement with ERIC

## Slide 31
1950
1970
1990
2010
2030
2050
2070
2090
1950
1970
1990
2010
2030
2050
2070
2090
research, development needs education, training

## Slide 32: Nuclear Fission RI access right in Belgium
Free access for Education & Training in the frame of BNEN and association agreements
Free access for fundamental research (after evaluation)
Shared cost (in-kind / in-cash) for joint programmes (bilateral/multilateral)
Full cost for services action
Commercial access for commercial activities

## Slide 33: Other institutions in Belgium useful RI for Nuclear Fission
Von Karman Institute:
  CFD and Thermal-hydraulics highly instrumented facilities
  Turbo-machinery qualification test bancs
  3-D seismic test facility for HLM Sloshing study
LABORELEC
  Mechanical Testing laboratories for RPV and reactor internals
  LTO : Cable aging
IRE
  Radiochemistry facilities
  RadioIsotopes production procedures V&V facilities
Ondraf-Niras/Belgoprocess
  Waste conditioning & Mgt RI
  Decontamination & site restoration RI

## Slide 34: Issues for Nuclear Fission RI to be addressed at EC level
Access for students and trainees to Nuclear Fission RI for E&T : Common access rules are needed at European level to favour mobility of our students and young professionals
Financial support (partial) for operation costs Nuclear Fission RI in the infrastructure support funds
Open Marie-Curie financing to EURATOM programme
Certification of professionals at EU level to allow attraction and mobility between European RI’s
Help the streamlining and realisation of Future large research infrastructures needed at European scale and presently supported at national level